Profa Website + (Picture for file geometry)

T-Blue File:

-Cross section: Rectangular

(Maximum Flexibility and Durability, Even Stress Distribution, Enhanced Canal Contact, Effective Debris Removal)

-Heat treatment: blue heated

(Blue Files are highly heat treated for best Flexibility and adaptability)

-Metallurgy: black NI-TI (CM wire)

(less carbon and oxygen impurities lead to maximum Durability)

- Dark Color coating (Provides better contrast against tooth structure)

-Opener and Glide path files have an active tip, while all shaping files has a non-active tip to avoid perforation and ledge formation

-Suitable for difficult or complex cases

severe curved canals or fine canals.

-Pack size: each pack contain six pieces

-Assorted: variety of option available in the product

-length range: lengths vary between 25 to 31 units

-Speed: 350-400 rpm

-Torque: 2.5 N/cm, 1.5 N/cm navigate

Eli-Gold File:

-Cross section: Each File has suitable cross section

- Opener (Angled Triangle) strikes a balance between flexibility, cutting efficiency, and durability.

- Glide path (Rectangular) Easier Canal Negotiation, Resistance to Fracture during initial steps.

- Shaping Files (Triangle) For better cutting efficiency

-Heat treatment: Gold heated NiTi

-Metallurgy: M Wire NiTi

- Spring back: the capacity of a bent file to revert to its original form.

-Incredible strength: higher cutting efficiency

-Opener and Glide path files have an active tip, while all shaping files has a non-active tip to avoid perforation and ledge formation

- Suitable for standard or simple cases, straight or fairly wide canals

-Pack size: each pack contain six pieces

-Assorted: variety of option available in the product

-length range: lengths vary between 25 to 31 units

-Speed: 300-350 rpm

-Torque: 3.0 N/cm Opener, 2.0 N/cm

Retreatment File:

-Three easily identified files are designed for the

different needs of un-filling the canal before

reshaping.

(D1: 16mm,9%) (D2: 18mm,8%) (D3: 22mm,7%)

- Material: NITI

- Gold plated M Wire

D1: for the removal of material from the coronal1/3.

Working Tip (D1) facilitates initial penetration

D2: for the removal of material from the middle1/3.

D3: for the removal of material from the apcial1/3.

Kiddo File:

-Specially designed for pediatric cases

- Material: NiTi

- Gold Plated M Wire

-All Files

Non-cutting Tip with Triangle cross section for better and faster cutting efficiency

Special Tip design (Small flat area) to avoid irritation & damage to the periapical tissue of primary teeth, and enhance its ability to find the way through the debris

Measuring 16mm (Best pick for kid’s root canal treatment)

Variety Tapering fits all primary canals (4%-6%)

-Sizes: 15-20-25-30

-Speed: 250-350 rpm

-Torque: 1.5N/cm

(Flower Endo stopper: measures working depth, Detachable petals to track the file usage and prevent cyclic fatigue, made of silicon and available in yellow color.

Advantages: -easy to set up, Fits all file, perfectly resistant to sterilization)

Manual files:

K-File:

-Strong and stable instrument for searching root canal cleaning and shaping

-Material: Stainless steel

-Size: ISO

-Length: 125mm

-Sterilization: 126

-Package: 6 pieces per box/blister

-Taper: 02

Spreader:

-Strong and stable instrument for Condensed the root canal obturation

-Material: Stainless steel

-Size: ISO

-Length: 125mm

-Sterilization: 126

-Package: 6 pieces per box/blister

-Taper: 02

Gates Glidden:

-Material: Stainless steel

-Size: ASSTD

-Length: 28mm

-Sterilization: 134

-Package: 6 pieces per box/blister

-Speed: 800

C-File:

-Strong and stable instrument used with Calcified Canals

-Material: Stainless steel

-Diameter: #8#10#15

-Length: 25mm

-Sterilization: 126

-Package: 6 pieces per box/blister

-Taper: 02

U-File:

-Strong and stable instrument used with ultrasonic instruments to wash the root canal

-Material: Stainless steel

-Diameter: #15#20#25

-Length: 33mm

-Sterilization: 134

-Package: 6 pieces per box/blister

-Taper: 02

-Cross section: Square