Tristar Website

Trubalance:

-A new generation of aligner material overcomes the difficulties by the (COMPOSITE SANDWISH TECHNOLOGY).

-Composite sandwich/polymer blend: A composite core with a TPU, yet outer shells are PETG.

-The elastic, central layer (TPU) allows the outer composite layers (PETG) to slide over each other, aiding extended elastic properties

-Consistent force delivery/stress retention over a 7 to 10-day period of wear, as over a 10-day period of simulated application, the clear aligner material can maintain up to 90% of the original force design, while current single layered materials lose up to 50% of their ability to deliver the same force over the first 8 hours of application of the aligner.

-Tristar will outperform all single layer aligner materials.

-Benchmark for CRACK RESISTANCE, as Tristar sheet was assessed as the highest for its “impact strength = 67.73Mpa” compare to other orthodontic material.

-Maximum elastic behavior, as Tristar sheet is able to stretch to almost three and a half times its original dimension before breaking (Material toughness = 350.98%)

-Minimal fluid behavior and superior chemical stain resistance and clarity.

-Suitable for all ages

-Package: Composite layered-aligner material

0.76mm x 125mm circle, 10 sheets/pack

T-Plus:

-The World’s First Material combine Functional appliances with Tooth movement capabilities.

-Use only for kids up to 10 years old

-Dual-COMPOSITE layer functional appliance  A hard, rigid outer layer to resist functional forces and a soft inner layer to perform tooth and root movement.

-The outer layer is a harder, high-strength polymer that provides the required biomechanical force for effective and predictable movement, while the inner layer consists of a softer, elastic polymer that improves comfort for pediatric and mixed dentition by minimizing pressure and irritation on gums and teeth.

-Total thickness of 1.8mm

-Main uses:

- Twin-block design aligner for mixed dentition case (kids), in which we have our own block design.

- Rapid Maxillary Expander (RME)

- Nightguard for sleep use

- Mandibular Advancement Device

-Package: Dual-layered Functional Appliance Material, 1.8mm x 125mm circle, 2 sheets/pack

Attachment Template:

-Temporary Thermoformed single-layer Ultra-precise fit sheet (0.3 mm)

- Tighter, thinner, and comfortable sheet that improves the attachment process.

-For the attachment template, usually we will print out around 2-4 sets for each patient, it can be used one time only normally, since our styles of bonding attachment is that we do it each tooth one by one.

-We will bond the attachment on the teeth one by one, since the template is cut, it can only use one time only.

-Package: Mono-layered Template Material, 0.3mmx125mm circle, 5 sheets/pack.

Valcon:

-Monolayered PET-G sheet Retainer

-Economical Solution, Thickest and stiffest option

-Highest stability and durability, Suitable for patients with parafunctional habits

-Package: Single Layered Temporary Retainer

1mm x 125mm circle, 25 sheets/pack

-Why dose Tristar material has a thin film on its surface?

: The thin film acts as a moisture barrier for Tristar material, a moisture-absorbing polymer, and helps prevent bubble and blister formation during thermoforming.

-What should be alert when using Tristar Material?

: All plastic sheets should be kept free from moisture after opening the pouch. Be sure to use the sheet within 15 min of the opening pouch.

-Which thermoforming machine suitable for Tristar?

: We recommend using advanced pressure-forming machines like BioSTAR, MiniSTAR, and Drufomat for improved gum line definition and gingival textures in thermoforming.